NS GROUT

Non-Metallic, Non-Shrink Grout

{Note to Specifier: This add-in specification component specifies Euclid Chemical Company, NS GROUT- Non-Metallic, Non-Shrink Grout.   NS GROUT is designed for critical use where high-strength, non-staining characteristics and positive expansion are required. NS GROUT contains only natural aggregate and an expansive cementitious binder. NS GROUT can be mixed and placed at fluid, flowable and plastic consistencies.}

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

1.1	QUALITY REQUIREMENTS

A.	Manufacturer: ISO 9001 quality certified as primary manufacturer of specified products.

1.2	INFORMATIONAL SUBMITTALS

A.	Product List: List manufacturer name and product name for each product proposed for use as cementitious grout.

B.	Manufacturer Certificate: Indicating products listed on Contractor's Product List are compatible and suitable for the specified application.

PART 2 - PRODUCTS

2.1	MANUFACTURERS

A.	Manufacturer: Provide listed products of Euclid Chemical Co., Cleveland, OH; www.euclidchemical.com.

B.	Manufacturer Single Source: Provide cementitious grout products from a single qualified manufacturer.

2.2	CEMENTITIOUS GROUT

A.	Cementitious Grout:  Cementitious grout for high performance applications.

1.	Product shall conform to:

a)	CRD C621, US Army Corps of Engineers Specification for Non-Shrink Grout

b)	ASTM C1107, Standard Specification for Packaged, Dry, Hydraulic-Cement Grout (non-shrink)

2.	Basis of Design Product:

a)	“NS GROUT” by The Euclid Chemical Company

b)	Flow rate, ASTM C939/CRD C621 @75oF (24oC), 50% RH:

1)	Flowable consistency, 1 gal./50 lb (3.8 L/22.7 kg)

a)	120% (Flow Table)

2)	Fluid consistency, 1.2 gal./50 lb (4.5 L/22.7 kg)

a)	23-30 seconds (Flow Cone)

c)	Compressive Strength, ASTM C109 Modified to ASTM C1107 Section 11.5, 2 in. (5 cm) cubes @ 75oF (24oC), 50% RH):

1)	Flowable consistency, 1 gal./50 lb (3.8 L/22.7 kg)

a)	3 days: 4500 psi (31 MPa)

b)	7 days: 6000 psi (41 MPa)

c)	28 days: 8500 psi (59 MPa)

2)	Fluid consistency, 1.2 gal./50 lb (4.5 L/22.7 kg)

a)	3 days: 3500 psi (24 MPa)

b)	7 days: 5000 psi (34 MPa)

c)	28 days: 6800 psi (47 MPa)

d)	Expansion, CRD C621 @ 75oF (24oC), 50% RH):

1)	Flowable consistency, 1 gal./50 lb (3.8 L/22.7 kg)

a)	3 days: 0.02%

b)	7 days:  0.02%

c)	14 days: 0.03%

d)	28 days:  0.03%

2)	Fluid consistency, 1.2 gal./50 lb (4.5 L/22.7 kg)

a)	3 days: 0.01%

b)	7 days:  0.03%

c)	14 days: 0.05%

d)	28 days:  0.05%

e)	Setting time @75oF (24oC), 50% RH:

1)	Initial set: 3 to 5 hours

2)	Final set: 4 to 6 hours

PART 3:	EXECUTION

{Note to Specifier: This section covers surface preparation, form preparation, mixing, placement, curing, and cleanup for Euclid Chemical’s NS Grout. For complete current instructions and safety information, consult the Technical Data and Material Safety sheets posted at www.euclidchemical.com. Note: The contractor and engineer are encouraged to consult and review the Euclid Chemical bulletin: “Cementitious Grout Application Guide”: (http://euclidchemical.com/fileshare/ProductFiles/MiscProductFiles/grout_instructions.pdf.)

The document offers instructions detailing the general installation of Euclid Chemical manufactured cement-based grout products. Important: If the contractor is not familiar with standard grout placement techniques, a pre-job meeting is suggested to review the project details unique to the particular job. Contact your local Euclid Chemical representative for additional information.}

3.1	SURFACE PREPARATION

A.	All surfaces to be in contact with grout shall be clean and free from rust, grease or oil.

B.	Saturate area to be grouted with water until it is uniformly damp. Remove excess water just before placing grout.

3.2	MIXING

A.	All grouting materials shall be 50°F to 80°F (10°C to 27°C) immediately prior to mixing.

B.	Mix grout in accordance with manufacturer’s written instructions. Mix small quantities with a drill and "jiffy" mixer. Use a paddle type mortar mixer for large jobs.

C.	Charge mixing vessel with appropriate amount of clean, potable water for batch size and then add dry grout. Do not exceed water content recommended by manufacturer. Control water content. Do not add admixtures, sand or cement to grout.

D.	Mix for a minimum of 2 to 3 minutes.

E.	Check flow.

3.3	PLACEMENT

A.	Place grout in accordance with manufacturer’s written instructions.

B.	For pouring, allow a minimum clearance of 2" (50 mm) for entry and 6" (150 mm) minimum grout head. On placing side, slope form to assist in grout movement and to prevent trapping air. Do not have close fitting forms. Allow 1" (25 mm) horizontal clearance and 1" (25 mm) vertical clearance for height above bottom of the baseplate. Forming must provide venting. Do not entrap air.

C.	Placed mixed grout immediately and continuously. Use rod or strapping to assist in placement if required.

3.4	FINISHING

A.	Finish grout in accordance with manufacturer’s written instructions. Remove forms as soon as grout has stiffened or set sufficiently to prevent sagging away from the bottom of the baseplate. Cut back shoulders and finish to desired texture where required.

B.	Pond with water or cover with wet rags, burlap or plastic to prevent premature drying as soon as sheen of water disappears and grout attains initial set.

3.5	CURING

A.	Cure grout in accordance with manufacturer’s written instructions.

B.	Following cut back, seal all surfaces with two (2) coats of a high solids curing compound. Alternately, keep all surfaces wet with water; covering with burlap or polyethylene for minimum of 72 hours.

3.6	CLEAN UP

A.	Tools and mixer may be cleaned with water.