EUCO ROCK

Rapid Setting Flowable Grout

{Note to Specifier: This add-in specification component specifies Euclid Chemical Company, EUCO ROCK RAPID SETTING FLOWABLE GROUT. EUCO ROCK is designed for anchoring or grouting applications. EUCO ROCK contains only natural aggregate and an expansive cementitious binder. It contains no mettalic aggregate or added chloride. EUCO ROCK sets rapidly and achieves load-bearing and bond strengths.}

{Note to Specifier: The paragraphs below are meant to be incorporated into Parts 2 and 3 of a standard CSI 3 Part Format specification, project’s General Structural Notes or directly onto the plans. They must be carefully reviewed by a qualified design professional and edited to meet the particular requirements of the project at hand, assure compliance with any governing building codes, and coordinate with other specification sections and drawings.}

1.1	QUALITY REQUIREMENTS

A.	Manufacturer: ISO 9001 quality certified as primary manufacturer of specified products.

1.2	INFORMATIONAL SUBMITTALS

A.	Product List: List manufacturer name and product name for each product proposed for use as cementitious grout.

B.	Manufacturer Certificate: Indicating products listed on Contractor's Product List are

compatible and suitable for the specified application.

PART 2 - PRODUCTS

2.1	MANUFACTURERS

A.	Manufacturer: Provide listed products of Euclid Chemical Co., Cleveland, OH;

www.euclidchemical.com.

B.	Manufacturer Single Source: Provide cementitious grout products from a single qualified manufacturer.

2.2	CEMENTITIOUS GROUT

A.	Cementitious Grout:  Cementitious grout for high performance applications.

1.	Basis of Design Product:

a)	“EUCO ROCK” by The Euclid Chemical Company

b)	Compressive Strength, ASTM C109, 2 in. (5 cm) cubes @ 72oF (22oC), 50% RH):

1)	3 hours: 2600 psi (17.9 MPa)

2)	24 hours: 3800 psi (26.2 MPa)

3)	7 days: 5000 psi (34.5 MPa)

4)	28 days: 6000 psi (41.7 MPa)

PART 3 - EXECUTION

{Note to Specifier: This section covers surface preparation, form preparation, mixing, placement, curing, and cleanup for Euclid Chemical’s EUCO ROCK. For complete current instructions and safety information, consult the Technical Data and Material Safety sheets posted at www.euclidchemical.com.  Note: The contractor and engineer are encouraged to consult and review the Euclid Chemical bulletin: “Cementitious Grout Application Guide”:

(http://euclidchemical.com/fileshare/ProductFiles/MiscProductFiles/grout_instructions.pdf.

The document offers instructions detailing the general installation of Euclid Chemical manufactured cement-based grout products. Important: If the contractor is not familiar with standard grout placement techniques, a pre-job meeting is suggested to review the project details unique to the particular job. Contact your local Euclid Chemical representative for additional information}

3.1	SURFACE PREPARATION

A.	All surfaces to be in contact with grout shall be clean and free from rust, grease or oil.

B.	Saturate area to be grouted with water until it is uniformly damp. Remove excess water just before placing grout.

3.2	MIXING

A.	All grouting materials shall be 50°F to 80°F (10°C to 27°C) immediately prior to mixing.

B.	Mix grout in accordance with manufacturer’s written instructions. Mix small quantities with

a drill and "jiffy" mixer. Use a paddle type mortar mixer for large jobs.

C.	Charge mixing vessel with appropriate amount of clean, potable water for batch size and then add dry grout. Do not exceed water content recommended by manufacturer. Control water content. Do not add admixtures, sand or cement to grout.

D.	Mix for 1 minute.

3.3	PLACEMENT

A.	Place grout in accordance with manufacturer’s written instructions.

B.	Placed mixed grout immediately.

3.4	FINISHING

A.	Finish grout in accordance with manufacturer’s written instructions. Cut back grout and finish to desired texture where required.

3.5	CURING

A.	Cure grout in accordance with manufacturer’s written instructions.

3.6	CLEAN UP

A.	Tools and mixer may be cleaned with water.